Chapter 7

NON-TRADITIONAL PROCESSES

- WATER JET MACHINING (WJM)

## (SU JETİ İLE İŞLEME)

Figure 1.1 Principle of WJM

Figure 1.2 Nozzle

Common Use

-Used to cut and slit porous non-metals (started in 1971 in the USA)

-Nozzle diameter of d=0.1 - 0.25 mm (Figure 1.2).

-No abrasive particles are used.

# Mechanism of Material Removal

In the first few milliseconds after the initial impact of the jet on the workpiece (before the lateral flow is initiated), a transcend pressure of three times the normal stagnation pressure is generated (Figure 1.1). Erosion occurs when the local fluid pressure exceeds the material's strength.

# Typical Pressures and Velocities

Psupply = 350 MPa (range: 70 - 700 MPa, typically 400 MPa)

Pstatic = 350 MPa

Phammering = 1000 MPa

(yield)steel = 400 - 700 MPa

Vflow= 300 - 900 m/s

Nozzle (Figures 1.2 and 1.5)

Nozzle material should be extremely hard. Typical materials;

- Sintered diamond,

- Sapphire (synthetic),

- Tungsten carbide,

- Special steels.

The diameter typically ranges from 0.07 to 0.5 mm. Nozzle lifetime is 250-500 hrs.

To increase the length of the coherent jet (Figure 1.5b) (i.e., without dispersion), ~1% long-chain polymer is added to water to increase the viscosity of water. In this way, length/diam=600 can be obtained.

Due to the table movement, the jet angles cause angled traces on the workpart (Figure 1.6).

| a) |  |
| --- | --- |
| b) |  |

Figure 4.5 Nozzle and the Coherent Jet

Figure 1.6 Deflection of Jet Due to Table Movement

# Applications

|  | -Wood industry (for cutting purposes), |
| --- | --- |
|  | -Cutting brick and marble (Figure 1.7e, 1.7g, 1.7h), |
|  | -Paper industry (corrugated box board cutting) (Figure 1.7i), |
|  | -Textile (confection) industry, |
|  | -Leather, |
|  | -Coal mining, |
|  | -Fiberglass and polyethylene automotive parts (by using robots), |
|  | -Cable stripping, |
|  | -Thin Metal cutting (Figure 1.7a-1.7d, 1.7f, 1.8, 1.11). -Glass cutting (Figure 1.9) |

| a) |  | b) |
| --- | --- | --- |
| c) |  |  |
| d) |  | e) |
| f) |  | g) |
| h) | i) |  |

Figure 1.7 WJM Application Examples

Figure 1.8a Aluminum Cutting

Figure 1.8b Steel Cutting

Figure 1.9 Glass Cutting

Figure 1.10 Tomato Cutting

Figure 1.11 Turbine Blade Cutting

Figure 1.12 A Large-Scale Work

# Technical Capabilities

Cutting up to 250 mm thickness (then, the jet diverges)

# Advantages

|  | -No problem about nozzle wear compared to AJM, |
| --- | --- |
|  | -No heat damage, |
|  | -Cutting can start at any location, |
|  | -Gives clean (dust-free) and sharp cut (minimum kerf), |
|  | -Water is cheap, available and non-toxic, |
|  | -High cutting rates. |

Machine Tool (Figure 1.13)

Figure 1.13 WJM Machine Tool

Figure 1.14 PC Control Screen

2. ABRASIVE WATER JET MACHINING (CUTTING) (AWJM) (AŞINDIRICILI SU JETİ İLE KESME)

Commonly used abrasives:

Garnet

- It is the most common type of waterjet abrasive.

- Hard and sharp. Ideal for cutting through hard materials.

- Produces a smooth finish.

- Relatively inexpensive.

### ➣ Silica Sand (SiO2)

- Less expensive than garnet.

- It can be used to cut through soft materials.

- Produces a rough finish.

- Softer than garnet. It may not be suitable for cutting through hard materials.

### ➣ Aluminum Oxide (Al2O3)

- Harder than garnet. Ideal for cutting through very hard materials.

- Produces a smooth finish.

- More expensive than garnet.

Figure 2.1 Nozzle Principle

Figure 2.2 Schematic Presentation of Abrasive Mixing in the Nozzle

| Figure 2.3 AWJM Nozzle Cross-section | Figure 2.4 Nozzle |
| --- | --- |
| Figure 2.5 AWJM Machine Tool |  |
| Figure 2.6 Grate Table | Figure 2.7 Nozzle |
| Figure 2.8 Pinion And Rack Cut By AWJM -------------------------------------------------------------------------------------- |  |

3. ELECTRIC DISCHARGE MACHINING (EDM)

## (ELEKTRO EROZYON İLE İŞLEME)

# Applications

Lazarenko (1943) discovered the erosive effects of electric discharges. Usage is favorable for

- Hard metals or alloys which conventional techniques cannot machine

- Very complex shapes.

Figure 3.1 Electric Discharge Machining

# Mechanism of Metal Removal

When a voltage is applied between the electrodes, an electric field builds up. Electrons are removed from the cathode surface and impelled towards the anode due to the electric field (Figure 3.1). During their travel, they collide with neutral molecules of the dielectric, detaching electrons and causing ionization. Since the channel is narrow, a continuous current flows (electrons moving along the channel to the anode). Due to increased channel temperature, the fluid evaporates, increasing the flow density. The discharge temperature in the channel is 8.000 - 12.000º K. This causes fusion (melting) or partial evaporation of metal and dielectric at the discharge point. The metal in liquid drops is dispersed in the dielectric due to the explosive pressure of gaseous products in the discharge (Figure 3.2a and 3.2b).

(a)

(b)

Figure 3.2 a) Crater Removed by a Plasma Channel ("1" evaporated (100% removal, "2" boiled (70-80% removal), "3" melted (18 - 20% removed)),

b) Crater formed by a single spark on a ground surface

The popularity of the EDM process is due to the following advantages;

|  | - For electrically conductive materials (physical and metallurgical properties are not effective) |
| --- | --- |
|  | - No physical contact (no mechanical deformation) |
|  | - There is a slight thermal effect on the surface; the bulk of the material is not even heated. |
|  | - Complex shapes can be produced with high accuracy. |
|  | - The surface is formed by craters (craters provide better lubrication in some applications). |
|  | - It needs very little operator attention. |

(a)

(b)

Figure 3.6 a) An industrial type EDM Machine Tool and Tank-Electrode Arrangements, b) A Big EDM Machine Tank (KAREL KALIP INC. Tuzla/İSTANBUL)

-------------------------------------------------------------------

## Functions and Properties of Dielectric Fluids

|  | -Remain electrically nonconductive until the required breakdown voltage is reached (i.e., it should have high dielectric strength). |
| --- | --- |
|  | -Breakdown electrically in the shortest time once the breakdown voltage is reached |
|  | -Provide an effective cooling medium |
|  | -Carrying away the swarf particles (work and electrode materials, decomposition products, hydrogen, carbon, bubbles) |
|  | -Good degree of fluidity |
|  | -Be cheap and readily (easily) available |

Typical Fluids (the size of particles in the dielectric is ~ 3 - 5 m)

|  | -Light hydrocarbon oils (transformer oil, kerosene, paraffin oil, and lubricating oils) |
| --- | --- |
|  | -Silicon-based oils |

## Typical Electrode Materials and Their Characteristics

80% of the money spent on EDM is due to the tool electrodes (their design, shaping and material) (Figure 3.9a). So, it must be chosen very carefully.

| Material | Wear | MRR | Fabrication |
| --- | --- | --- | --- |
| Copper | Low | High (for roughing) | Easy |
| Brass | High | High (for finishing) | Easy |
| Tungsten | Lowest | Low | Difficult |
| Tungsten Copper | Low | Low | Difficult |
| Cast Iron | Low | Low | Easy |
| Steel | High | Low | Easy |
| Zinc-based alloys | High | High (for roughing) | Easy |
| Copper Graphite | Low | High | Difficult |

| Tool Electrode Design (Figure 3.9). If there are three electrodes; |  |  |  |
| --- | --- | --- | --- |
| Electrode |  | Electrode #1 (smaller than the final cavity size) | Electrode #2 (near the final cavity size) | Electrode #3 (almost equal to the final cavity size |  |
| Metal Removal (%) |  | 80 | 18 | 2 |  |
| Machining Rates |  | High | Medium | Very low |  |

Figure 3.9 Overcuts Between Tool Electrode and Workpiece

# Figure 3.9a Some electrodes and their machined surfaces

# Surface Finish

|  | -Ra is 0.8 - 4 m (with special setup 0.2 m). |
| --- | --- |
|  | -The quality of the surface mainly depends on the spark's energy. If the energy content is high, deeper craters will produce a poor surface. |
|  | -Surface roughness is inversely proportional to discharge frequency (Ra ~ 1 / f). |

# Technical Capabilities

|  | -Accuracy =± 0.025 - ± 0.1257 mm. |
| --- | --- |
|  | -Taper= 0.0005 - 0.005 mm/mm |
|  | -H/D = Aspect ratio (when drilling small holes) = 30/1 |
|  | -MRR = 0.01 - 0.1 cm3/hr (finishing). MRR can be 15-20 times higher than finishing values in roughing operations. |

# Applications of EDM in Industry

It is reported that the use of EDM as;

|  | -50% die shops |
| --- | --- |
|  | -30% captive (demand-based) industrial tool rooms |
|  | -10 % aerospace |
|  | -5% automotive parts |
|  | -5% others The application fields (Figure 3.12a-12c) -Difficult (hard) to machine materials (electrically conductive),. -Deep cavities,. -Conical machining, die cavity sinking,. -Small holes, narrow slots,. -Micromachining (small scale),. -Repair work of dies, through holes,. -Complex shapes,. -Non-circular holes.. |

Figure 3.12a Some Applications of EDM

Figure 3.12b The EDMed Die Surfaces (KAREL KALIP INC.-Tuzla/İSTANBUL)

SME Video/Machining Processes

---------------------------------------------------------------------------------------------

4. WIRE EDM (WEDM)

## (TEL EROZYON İLE KESME)

a)

b)

Figure 4.1 Principle of WEDM, Movements of Wire and Workpiece

General Application

Applicable for 2D cutting processes. A wire is used instead of a shaped electrode in die-sinking EDM.

Machining Principles

- Wire (Figure 4.2)

d1>d2

d=0.15 - 0.3 mm for copper and brass wire

d=0.05 - 0.15 mm for molybdenum steel wire

Figure 4.2 Cutting Width (KERF) in WEDM

b) Dielectric

Dielectric is "deionized water".

- KERF (Figure 4.2)

a: KERF

x: spark gap (0.025-0.05 mm)

a = 2x+d

amin= 0.1 mm.

- Motions

-u and v  are the motions of the upper guide to the lower guide to cut in angle (u, v displacements are max. 35 mm distance) (Figure 4.1b).

-x, y, u and v movement axes are controlled by CNC.

-During machining (cutting), the table controls the movement route for replacing the wire-pushing.

Technical Capabilities

|  | -Linear cutting speed, Vx, Vy = 38 - 115 mm/hr |
| --- | --- |
|  | -Wire-speed = 8 - 42 mm/s |
|  | -Only for through cutting. |
|  | -Accuracy = ±0.007 mm (common) |

Figure 4.3 WEDMed Workpieces

SME Video/Machining Processes

5. LASER BEAM MACHINING (LBM) (CUTTING/DRILLING/WELDING)

## (LASER İLE İŞLEME (KESME/DELME/KAYNAK))

LASER (Light Amplification Using Stimulated Emission of Radiation)

Sun's radiation: 7 kW/cm2    (on the sun's surface)

In laser for short pulses: 10 kW/cm2    (on beam cross-section)

# Principles

-If a laser beam is focused on (1/100) of mm2, E=105 kW/cm2, this heat vaporizes any known materials.

-The laser rod is excited by a xenon-filled flash lamp that surrounds it.

E(usable) = 106 - 107 kW/cm2

Efficiency = Eusable / Esupply = 0.5 - 50 %

# Material Removal Mechanism

Melting and evaporation of the workpiece material under extensive heat

Solid-State LBM Mechanism (nowadays, instead of flash lamps, laser diodes are used due to their light efficiency).

Lasing materials for Solid-state lasers: Ruby, Er-YAG, and Nd-YAG laser rods.

(a)

5-DOF Laser Drilling Machine

(b)

Figure 5.1 LBM Mechanism

# Laser Types and Materials

| Continuous waves (CW) |  | Heavy and continuous machining |
| --- | --- | --- |
| Pulsed waves |  | drilling of small areas |
|  |  | for thin material (sheets) |

Laser materials and performances

| Laser Material | Wavelength (m) | Mean Power (W) |  (%) | Relative Cost |
| --- | --- | --- | --- | --- |
| CO2 (gas) | 10.2 | 100 - 25.000 (400 - 1.500 common) | < 10 | 400 |
| NdYAG (Continuous) * | 1.06 | Av. 400 (peak 20.000) | < 1 | 10 - 44 |
| Nd YAG (Pulsed) * |  |  |  |  |
| Argon (gas) | 351 - 529 | - | < 0.1 | 3 - 9 |
| CO (gas) | - | 2000 | 60 |  |

* Solid state of neodymium, yttrium-aluminum-garnet

Possibilities for Cutting (Figure 5.1a)

- Move the workpiece

- Move the laser equipment

- Move the lenses or mirror (the simplest way)

# Applications

- LBM Drilling

-Round holes ranging from 0.127-1.27 mm can be drilled.

-L/D ratios = 100/1

-Heat affected zone thickness = 0.002 - 0.1 mm

-Diametric repeatability = ± 0.025 mm (or 10% of the diameter)

Figure 5.2 Gas-assisted Laser Cutting

- LBM Cutting (Figure 5.2)

-LBM Cutting = (Laser beam) + high-velocity gas to melt, vaporize and oxidize (oxygen (highest cutting speeds), air, argon (to prevent oxidation),)

- Cutting stainless steel is extensive.

-Holes with a diameter larger than 10 mm or holes that are not round are produced by CNC contour cutting.

-Trepanning can produce holes with a 0.5-10 mm diameter range. L/D = 20/1 (Figure 13.3).

Laser trepanning              Hole trepanning              Micro hole trepanning.

Figure 5.3 Laser trepanning

Figure 5.4 LBM Cut Parts

Figure 5.4 (cont'd)

Wood engraving                          Stamp engraving                    Photo engraving

Cylinder item                               Metal engraving

Plastic engraving

Figure 5.5 Laser Engraving

- Laser Engraving (Figure 5.5)

Laser engraving (or laser marking) is the practice of using lasers to engrave or mark an object. The system is capable of engraving precisely on any metal and non-metal materials. YAG lasers (50-100W) and CO2 (80W/100W) are common. The engraving speed is 0-1000mm/s. Worktables are the electrical type with up and down movements.

- LBM Welding

## Used for spot and seam welding (Figure 5.6-a.). Weld penetration is limited to a maximum of 2.5 mm. Some seam welding and filling applications are shown in Figure 5.6-b

(a)

(b)

Figure 5.6 (a) Laser Welding Principle, (b) Laser Seam Welding and Filling Applications